88888888888888888888888                            JCPDS-NBS*LSQ82

A Least Squares Unit Cell Refinement Program

Camden R. Hubbard

Inorganic Materials Division

Center for Materials Science

National Bureau of Standards

Washington, D.C.   20234

and

Steven M. Lederman and Nikos P. Pyrros

JCPDS--International Centre for Diffraction Data

1601 Park Lane

Swarthmore, PA   19081

-1-

TABLE OF CONTENTS

PREFACE..........................................................ii

AVAILABLE COMPUTER PROGRAMS FOR X-RAY POWDER DIFFRACTION.........iii

INTRODUCTION.....................................................1

PROGRAM DETAILS..................................................3

Quantity Minimized...........................................3

Figures of Merit.............................................3

Systematic Error Test........................................5

Auto Indexing................................................6

Data Rejection...............................................7

PROGRAM EXECUTION

Batch Mode...................................................8

Batch Mode Input Card Descriptions and Formats..............10

Interactive Mode............................................17

Interactive Mode Input Description..........................18

PKS File Mode...............................................20

DEFAULTS........................................................21

EXECUTION ON NBS' UNIVAC 1182...................................22

REFERNCES.......................................................23

APPENDICES

A.   D-Spacing Generation Example

B.   Least-Squares Example

C.   PKS File Input Example

D.   PKS File Format

i

PREFACE

The computer program, JCPDS-NBS*LSQ82, was developed as part of the

cooperative program in x-ray powder diffraction between the JCPDS--

International Centre for Diffraction Data and the National Bureau of

Standards.  In addition to computer program development, outputs of the

cooperative program include high quality x-ray powder diffraction

refernce patterns, editorial review of data entering the Powder

Diffraction file (PDF), and critical evaluation of the current contents

of the PDF.  The JCPDS--International Centre for Diffraction Data

publishes the PDF, search indexes, selected subfiles, and related items.

For details of publications by the JCPDS--International Centre for

Diffraction Data, write to:

General Manager

JCPDS--International Centre for

Diffraction Data

1601 Park Lane

Swarthmore, PA   19081

Other computer programs available at NBS for x-ray powder

diffraction are listed below.  Related publications and/or

program listings will be sent upon request.  For details,

write to:

Dr. Camden R. Hubbard

A221/Matls

National Bureau of Standards

Washington, D.C.   20234

For a copy on magnetic tape, send a separate reel for each program

package (9-track, 1600 bpi, labeled).  The tape will be written in

ASC11 with multiple records per block.  Univac users may request

Copy, G format of symbolics, relocatables, and absolutes.  In all

cases, necessary data files and test decks are included.  All

programs are written in FORTRAN77 and are running on a Univac 1100

computer.

iii

AVAILABLE COMPUTER PROGRAMS FOR X-RAY POWDER DIFFRACTION

JCPDS-NBS*POWDER82.  (N.P. Pyrros and C.R. Hubbard)  This

package of programs is used to analyze digitally collected

powder patterns.  It includes background determination, second

derivative peak location, external standard 2 calibration, PKS

file creation and editing, as well as several plotting routines.

The PKS file provides tthe connectivity between modules and the

least-squares program, JCPDS-NBS*LSQ82.

NBS*QUAN82.  (C.R. Hubbard and R.L. Snyder) A package of programs

for general quantitive analysis by spiking, intensity ratio, or

internal standard methods.  Measurements of multiple lines and

multiple mountings can be used.  In the internal standard method,

overlapped lines and elemental analysis data can be included to

improve the XRD phase analysis.

AUTO.  (R.L. Snyder, C.R. Hubbard, and N.P. Pyrros) AUTO is an

interrupt driven, dual diffractometer control program.  It

permits collection of data for an entire pattern or from

selected regions.  The raw data file can be read directly by

JCPDS-NBS*POWDER82 and NBS*QUANT82.

NBS*AIDS83.  (C.R. Hubbard, J.K. Stalik,A.D. Mighell, and

M. Holomany)  This is a revision of NBS*AIDS80 for single

crystal and powder diffraction data evaluation, crystal data

cell calculation, hke/20/d-spacing generation, numerous data

consistency checks, least-squares refinement of lattice

parameters (subset of LSQ82), and figure-of-merit calculations.

JCPDS-NBS*LSQ82

A least Squares Unit Cell Refinement Program

INTRODUCTION

The determination of lattice parameters from x-ray powder

diffraction data is an important step in the characteization

of a crystalline phase.  X-ray powder diffraction data can

lead to cell parameters accurate to a few parts in 10,000 or

better (e.g., see NBS Monograph 25, Section 19, 1982).  Such

accuracy is achieved with measurement of peak locations to

within 0.01 20, internal standard calibration of 20, and,

finally, a least-squares refinement of unit cell parameters.

For nearly twenty years, the program of Evan's Appleman and

Hardworker (1973) has been widely used for this purpose.

There program is commonly referred to as the Geological

Survey program.  This report describes a new version of the

program which includes conversion to FORTRAN77 and major

revision of the program's input and output features.  Only

minor, special case revisions to their computational

segments were required.

The new program, JCPDS-NBS*LSQ82, provides for three

alternative modes of data input:  prompted free format

interactive input; formatted card image input; and reading

of a magnetic data file created by the JCPDS-NBS*LSQ82

system of programs (Pyrros and Hubbard, 1983).  The input

data are checked for consistency with the program

requirements.  Extinction conditions can be automatically

generated from the space group, aspect or centering

symbol.  In the formatted card image input mode, the unit

cell angles can be entered either as degrees in decimal

form or as degrees and minutes in integer form.  To

allow for reduction of printed output, often needed in

interactive computing, print options have been added.

The final listing was reduced in length by up to 50

percent and made more reliable by printing the author's d, 20,

and hk data on the same line as the program's generated d',

20', andh'k'e', when equivalent.  The calculation of figures

of merit by two methods has been added to enable the user to

evaluate the quality of the derived unit cell and the internal

consistency of the cell and observed data, respectively.

Several tests for the presence of systematic errors have also

been added.  These include the average of 2* calc 2* obs'

comparison of the number of lines with * greater than and

less than 0.02, and a statistical test for nonrandomness in

2* as a function of 2* (Hubbard and Stalick, 1982).

JCPDS-NBS*LSQ82 meets the requirements of ANSI standard

FORTRAN77.  The dimensions of large arrays can be readily

changed by revising the appropriate FORTRAN PARAMETER

statements in each routine.  As distributed, the maximum

number of observed lines (MAXOBS), the maximum number

of program generated lines (MAXGEN), and the maximum

number of lines in the peak file (MAXPKS) are set at 200,

1000 and 300, respectively.  With these array dimensions, the

code requires ???? words for data storage and ???? words for

program instruction on the UNIVAC 1100/82 (one word=36 bits).

Overlaying could reduce the storage required for program

instructions but would probably save little data storage.

The authors wish to acknowledge the helpful suggestions of

J. Stalick, E. Evans, H McMurdie, M. Morris, B. Paretzkin,

and B. Post.

-2-

PROGRAM DETAILS

Quantity Minimized

The Geological Survey program minimizes,

where *corr/hkl is the observed value of theta corrected for

instrumental and physical peak shifts (e.g., L* effects,

sample displacement, film shrinkage), *calc/hkl is the theta

value calculated from the current unit cell parameters, and

w/hkl is a weighting factor.  The corrections are readily

determined through use of 2* internal standard.  Since they

unit cell parameters are related nonlinearly with *calc, a

nonlinear least-squares refinement is used.  The Evans, Appleman,

and Handwerker (1973) paper fully describes details and

determination of the estimated standard deviations of the unit

cell parameters.

Figures-of-Merit

Both M20 (de Wolff, 1968) and FN (Smith and Snyder, 1979)

figures-of-Merit are calculated by the program.  M20 is defined

by,

where Q=1/d2, Q20 is the value of Q for the 20th observed line (not

counting unexplained lines), N20 is the number of different calculated Q

values up to Q20, and is the average magnitude of the discrepancy in Q

for these 20 lines.  The number of unindexable lines occurring, up to

the 20th observed and indexed line, is X20.  A value of M20 10 will

guarantee the essential correctness of the indexing provided these are

not more than two spurious lines (X20<2) [de Wolff, 1968].

FN is defined by,

Where n is 30, or the maximum number of lines of the pattern if the

entire pattern has fewer than 30 lines. Nposs is the number of

diffraction lines allowed in the space group, up to the nth observed

and indexed line.  Co-positional lines, such as the cubic 221 and 300,

are counted as on possible line. HKL is the average absolute magnitude

of the difference between the corrected and calculated 20 values for

each reported hkl for the first N lines.  FN thus indicates the

accuracy and completeness of the data.  The format for reporting the

Smith-Snyder figures of merit is FN(  ,Nposs).  Values reported in

NBS Monograph 25, section 18, range from F30= 17.6(0.017,99) toF10=

121.6(0.008,10).

If the user assigns two sets of indices to a single observed line

(multiply indexed line), then the equations for M20 and FN can be

implemented in two ways.  One can choose the set with smaller*20

and ignore the other set.  Alternately, both  *hkl and *hkl can

be included in the average.  The latter approach was chosen for

NBS*AIDS80 (Mighell, Hubbard, and Stalik, 1980) and implemented in

JCPDS-NBS*LSQ82.  This yields a lower figure-of-merit when two or

more hkl values are assigned to a *corr value  Another problem

which involves determination of Nposs can lead to different values

of M20 and Fn depending on program implementation.  The definition of

Nposs is the number of space group allowed lines out to *N.  To

allow for the possibility that *calc hkl>n hkl and than nposs then

would not include the calculated line hkl requires to index *N hkl

an increment of 0.025 is added to N prior to counting Nposs.

Systematic Error Tests

The possiblity os systematic errors in 20 corr is tested in three

ways:  (1) average*20 (=20 corr -20 calc); (2) number of lines with

*20 greater than +0.02 and less than -0.02; and  (3) a statistical

test.  All three tests use only the lines indexed at the end of the

final d/hkl/20 table.  If given an input line was assigned multiple

sets of hkl, then the *20 for each hkl is used just as in the

calculationof figures-of-merit.

The statistical test is based upon the paper, "On Randomness in

Ordered sequences", by young (1941).  He shows that when,

and,

then, statistically, the *20 ordered sequence of *20 values is not

randomat the 95 percent significance level if c/o > 1.645 and at

the 99 percent level if c/0>2.326.  To apply Young's equation to

the *20 ordered sequence of *20 differences, let,

and

In the powder diffraction case, when**i/n=* is non-zero, systematic

errors are likely.  For least-squares refined cell parameters, * is

essentially zero.  Thus, we have refined c to be,

so that *c/o will be larger when * is non-zero.  One drawback of the

*c/o test is that it is quite sensative to inclusion of a misindexed

line (large****).  It also can give an indication that systematic

errors are present in the data when all ** are small and the sequence

of * values is not important.

Auto Indexing

Often a user will have a trial cell and a set of corrected *20

values.  The program can be used to assign sets of *hkl to the *20

values.  This is often called Auto Indexing.  Because lower *20

reflections can be assigned *hkl sets more easily than at higher

*20, the program only assigns sets of *hkl for reflections below

THTMX for the first NCYC cycles of cell parameter refinement.  All

reflections index  will have *20 less than TOL is initially set to

TOLMX.  TOL is automatically adjusted after each cycle to two times

the standard error of a unit weight observation for TOLMN, which

ever is larger.  After the NCYC cycles, the program attempts to

index all reflections.  If a reflection cannot be indexed with *20

<TOL, then it remains unindexed.

Auto indexed reflections do not contribute to the least-squares

equations if the indexing choice is not unique.  Such cases are

flagged with an 'M' in the final llisting (See test B1) when (a)

the observed *20 is within TOL of the generated *20; (b) a second

generated *20 corresponding to the auto indexed line; or (c) two

observed *20 are within TOL of each other.

Data Rejecrion

User indexed reflections will not contribute to the least-squares

equations if the *20 exceeds TOL.  These refections

are flagged with an 'R' (*e.g.,in test 01, the )  the 1 2 2 at 34.770

has *20 =0.046, while TOL on the final cycle is 0.040).  Reflections

which are obviously misindexed on input  (**20>0.3deg.), as compared

to the generated *20 based on the input lattice parameters, are set

to unindexed (*hkl flag U).  The program will attempt to assign a

new set of hkl, as discussed above under Auto Indexing.  When this case

occurs, a "BAD HKL" message is printed. If an input set of hkl; are

not allowed by the systematic extinctions, the hkl flag is set to "U",

and then the reflection is considered unindexed.  Such lines may be

assigned an hkl set by the auto indexing feature.

-8-

PROGRAM EXECUTION

Three modes of data input are allowed by JCPDS*LSQ82:  batch,

interactive, and PKS file input.  Upon initiation of the program,

the prompt message, "ENTER:  TITLE, DEMAND, PKFILE, OR FINISH"

allows selection of input mode.  TITLE would signal that the input

is to be formatted by card images (usually used for batch mode

execution).  DEMAND would signal that free formatted input is to

be used  (usually for interactive use).  PKFILE would indicate

that a PKS file created by the powder pattern analysis package

JCPDS-NBS*POWDER82 is to be read.  Multiple problems can be run

one after the other.  FINISH terminates all input.

Details of the input data for each of the three modes are

given in the following three sections.

Batch Mode

The input of data via card images with formatted fields for

each possible input parameter was the only input mode allowed by

the original Geological Survey program.  This type of input is

often referred to as "batch" input and typically involves punched

cards.  Two additions to the batch mode input are of particular

importance.  First, lattice parameters are input on either a

"PARAM" or "PARAMD" card type.  The former requires angles in

degrees and minutes integer form, while the latter requires

degrees in decimal form.  The second modification was to allow

space group, aspect or centering symbol input via a SPACEG

card to simlify entering hkl* extinction condition information.

Input of the extinction condition information is still possible

on a SYSEXT card.   Only one of each pair ( PARAMD or PARAM

SPACEG or SYSEXT) should be included for each problem.  The

card formats are described in detail in the next section.

end -9-

-10-

Batch Mode Input Card Descriptions and Formats

Type of        Column     Format      Variable  Description

Card           Nos.

TITLE          1-6        A-6         ITEST     The word TITLE

with column 6

blank.

7-80       A74         IHEAD     Any alphanumeric

information de-

sired in heading.

PARAMD or                                       **Note only the

PARAM                                           unique lattice

parameters should

be entered.

System unique parameters

CUBIC  a

TETRA  a and c

ORTHO  a,b, and c

MONOC  a,b,c, and beta

RHOMB  a and alpha

HEXAG  a and c

HEXAR  a and c

PARAMD         1-6        A6          ITEST     The word PARMD

7-15       F9.6        AO(1)     Unit cell length a

16-24      F9.6        AO(2)     Unit cell length b

25-33      F9.6        AO(3)     Unit cell length c

34-41      F8.3        ALO(1)    Angle alpha in degrees

42-49      F8.3        ALO(2)    Angle beta in degrees

50-57      F8.3        ALO(3)    Angle gamma in degrees

58         II          ITTH      Flag for data input

=1 for theta

=2 for 2-theta

59-61      F3.0        THTMX     Angle limit in degrees

used for first NCYC

cycles for indexing

observations (default

=40 degrees 2-theta).

62         II          NCYC      Number of cycles during

which non-indexed

reflections with angles

exceeding THTMX are

not accepted in least-

squares solution.  If

NCYC is given as zero or

blank, a default value

of 2 is assigned by the

program.

63-67      	F5.4        TOLMN       Minimum tolerance used

in accepting reflections

(Default =0.03 in

2-theta).

68-72       F5.4        TOLMX       Starting tolerance used

in accepting reflections

(Default =5.0*TOLMN)

73          IT          IPHKL       Flag for print control:

=0 for print everything

=1 for do not print re-

flection data for each

cycle (i.e., print only

a summary following each

cycle).

74          	IT          IXPD        Flag for final table

printing:

0=for print

=1 for do not print

75            IT          NOINDX      Flag for use of input

hkl indexes:

0=use each hkl set input

1=consider every line

unindexed

76-80          F5.3        RESOLV      2-theta difference

between two generated

lines in order to be

considered resolved

(Default =0.075 in

2-theta)

Type of    Column     Format      Variable    Description

Card        Nos.

PARAM      1-6        A6          ITEST       The word PARAM (alter-

nate format to PARAMD

input)

7-15       F9.6        AO(1)       Unit cell length a

16-24      F9.6        AO(2)       Unit cell length b

25-33      F9.6        AO(3)       Unit cell length c

34-36      I3          IDG(1)      The number of degrees

in the angle alpha

37-41      F5.3        FMN(1)      The number of minutes

in the angle alpha

42-44      I3          IDG(2)      The number of degrees in

the angle beta

45-49      F5.3        FMN(2)      The number of minutes in

the angle beta

50-52      I3          IDG(3)      The number of degrees in

the angle gamma

53-57      F5.3        FMN(3)      The number of minutes in

the angle gamma

58-79                              See instructions for

PARAMD

SPACEG    1-6    A6     ITEST    The word SPACEG

7-11   A5     ICRYST   Choose one of the following:

CUBIC, TETRA, ORTHO, MONOC,

RHOMB, TRICL, HEXAG, OR

HEXAR

NOTE: HEXAR must be used for

rhombohedral lattice on hex-

agonal axes.

12-14  F3.0   THEMX    Limit of 2-theta for generating

hkl.  Defaults are:  (1) 179 deg.

for hkl  generation; (2) maximum

2-theta observed +0.5 deg. for

least-squares refinement.

Type of     Column    Format    Variable      Description

Card        Nos.

15-20     F6.5      PWL           Alternate field for

lamba retained for

compatibility with

old desks.  See

columns 50-80.)

21-22      2x                      Blank

23-30      8A1      ISGI           Space group, aspect,

or centerin symbol

(e.g., P21/a or Fm3m).

The systematic extic-

tions automatically

generated from the

symbol.  The allowed

31-49      19x                     Blank

50-60      F11.6     PWL2          Primary field for

Lambda.  If>0, this

value is used no

matter what is in

columns 15-20.  If

both 15-20 and 50-

60 are left blank,

then the default

value, 1.5405981 A,

is used.

61-62     I2     IWTYP             =0 for use input

weights   =1 for

use unit weights

=2 for use Hess'

weights (Hess', 1951)

63-64     I2     IWCYC             Number of cycles to

use weights before

all are reset to 1.0.

A zero implies use of

weights according to

IWTYP for all cycles

65-80    	16x                      Blank

Type of    Column     Format     Variable    Description

Card       Nos.

SYSEXT     1-6        A6         ITEST       The Word SYSEXT

(alter-

nate for

SPACEG)    7-14                              See instructions for

SPACEG card

21-47       IOP(1) to IOP(47)      In any column, enter the

inclusive              specific value for B (2,3,

4, or 6) which satisfies

the reflection condition

assigned to that column

Class of  Conditions for

Reflec.   Non-extinction

21          I1                       hkl     h+k=Bn

22          I1                       hkl     h+l=Bn

23          I1                       hkl     h+l=Bn

24          I1                       hkl     h+k=Bx, h+l=By,

k+l=Bz (x,y,z

are any integers)

25          I1                       hkl     h+k+l=Bn

26          I1                       hkl     -h+k+l=Bn

27          I1                       hhl     h=Bn

28          I1                       hhl     l=Bn

29          I1                       hhl     h+l=Bn

30          I1                       hhl     2h+l=Bn

31          I1                       Okl     K=Bn

32          I1                       Okl     l=Bn

33          I1                       Okl     k+l=Bn

34          I1                       hOl     h=Bn

35          I1                       hOl     l=Bn

36          I1                       hOl     h+l=Bn

-14-

Type of     Column     Format     Variable   Description

Card        Nos.

Class of  Conditions for

Reflec.   Non-exticntion

37         I1                    hkO       h=Bn

38         I1                    hkO       K=Bn

39         I1                    hkO       h=k=Bn

40         I1                    hhO       h=Bn

41         I1                    hOO       h=Bn

42         I1                    OkO       k=Bn

43         I1                    OOl       l=Bn

44         I1                    hll       h=Bn

45         I1                    hll       l=Bn

46         I1                    hll       h+l=Bn

47         I1                    hll       h+2l=Bn

48-49      2x                    Blank

50-72                            See instructions for

SPACEG card

REFLECTION     1-3        A3                    Blank or HKL

4-6        3x                    Blank

7-11       15     IH(I,1)        h index (see below)

12-16       15     IH(I,2)        k index (see below)

17-21       15     IH(I,3)        l index (see below)

Type of     Column     Format      Variable  Description

Card        Nos.

NOTE: h, k, and l are

optional on any 2-theta

card.  If left blank,

computer will attempt to

assign hkl's.  User

assigned hkl remain

fixed for all least-

squares cycles.

22-30      F9.6        DSP(I)    d-spacings*

31-38      F8.6        WL(I)     Alternate lambda--

used to override

value on SYSEXT

card or default value.

Thus one can leave a

blank here for k*a2

here for specific re-

flections.  Non-zero

WL applies only to the

card on which it is

entered.

39-47      F9.5        OBSTH(1)  The bragg angle 2-theta

in decimal degrees*

END         1-3        A6          ITEST     The word END with blanks

in columns 4, 5, and 6.

Indicates end of a prob-

lem.  A new problem may

follow.

FINISH      1-6        A6          ITEST     The word FINISH. This

card is used only once,

after the END card of

the  last problem.  It

is the signal that there

are no more problems.

*Enter either d-spacing or Bragg angle 2-theta, but not both for the

same reflection.

Interactive Mode

Control parameter and data input via an interactive terminal is

also provided by the program upon entering the responce DEMAND.

In this mode, the program uses free format input.  That is, if a

list of items is requested, the user enters the items separated by

a comma or a blank.  To accept the default value, a slash ("/") is

entered.  Each user input is prompted by the program.  The meaning

of each particular variable was defined under the section, BATCH

MODE INPUT DESCRIPTIONS AND FORMATS.  This mode is frequently used

to generate a listing of possible 2*'s for a known cell and space

group (often referred to as "d-gen").  After entering the crystal

system, only the unique initial lattice parameters are requested.

Interactive Mode Input Description

All numerical inputs are free format.  Separate numbers in a list

by a space or comma.  A "/" is used to skip entry and accept de-

fault values.

Prompt Message          Variable   Responce

ENTER: TITLE, DEMAND    ITEST      DEMAND

PKF FILE, or FINISH

ENTER HEADINGS (A68)    IHEAD      Any alphanumeric title information

--68 characters

ENTER CRYSDTAL SYSTEM    ICRYST     CUBIC, TETRA, ORTHO, MONOC,

CODE (A5)                           RHOMB, TRICI, HEXAG, HEXAR

ENTER a (free format)    AO(1)      Unit cell length a

ENTER b*                 AO(2)      Unit cell length b

ENTER c*                 AO(3)      Unit cell length c

ENTER alpha*             ALO(1)     Unit cell angle alpha

ENTER beta*              ALO(2)     Unit cell angle beta

ENTER gamma*             ALO(3)     Unit cell angle gamma

ENTER PARAMETER INPUT FLAG  ITYPE      1 for theta

2 for 2-theta

3 for D-spacing

IS A LEAST-SQUARES TO BE        Y for yes

DONE?                           N for no

ENTER: NCYC, THTMX, TOLMN,      See PARAMD card.  A "/" is used

TOLMX, and RESOLV               to accept default values

ENTER:IWTYP, and IWCYC          See SPACEG card.  A "/" is used

to accept default values

ENTER: 2-THETA-MAX, IPHKL,      See SPACEG card.  Note that 2-

IXPD, PWL2                      THETA-MAX or THETA MAX is re-

quested, based in ITYPE

*Only the unique parameters are requested.

Prompt Message          Variable    Responce

ENTER: SPACE GROUP,     SPGI        See NBS TECH Note 1141, Appen-

ASPECT or CENTERING(A8)             dix A.  First character in upper

case. All other numeric or

lower case alphabetic (a,b,c,

d,m, or n)

ENTER:

THETA, hkl, WEIGHT, LAMBDA;         Input reflection data.  The

2-THETA, hkl, WEIGHT, LAMBDA; or    choice of theta, 2-theta, or

D-SPACING, hkl, WEIGHT, LAMBDA      d-spacing is selected by input

flag ITYPE(see above). A0.0

in the first field terminates

data input. A "/" after any

value is acceptable.  For ex.

to input only the 2-theta value

20.0; enter 20.00/

PKS File Mode

In the PKS file input mode (PKFILE), a computer file created

by the JCPDS-NBS*PATTERN82 system of programs is read.  This file

contains all the parameters (e.g., cell, space group, 20's*, etc.)

needed by JCPDS-NBS*LSQ82.  The reflections in the file are marked

to be used or not to be used in the least-squares refinement.  Re-

flections flagged as "not to be used" are, however, compared with

the final list of possible reflections.  If a possible reflection

and a "not to be used" observation closely fit, this is noted in

the final listing.  This feature permits use of well resolved, strong

reflections for a preliminary cell parameter refinement.  Then, when

weak peaks are clearly indexed, they can be marked "to be used" in

least-squares refinement and the program rerun.  An example of this

program mode is given in Appendix C.  The PKS file format is given

in Appendix D.

DEFAULTS

The following conditions or constants apply for all input modes

unless non-zero values are entered.

1.   If input is in terms of 2-theta, output will also be in 2-theta.

Input of "d's" is OK; output then is in 2-theta by default.  If

out put is in theta, output will be in theta; for this option,

it is necessary to set ITHT=1 on the PARAM or PARAMD card, col. 58,

format I1.

2.   Lambda= 1.5405981 A.

3.   Reflections greater than 2*=40.0 deg. are not used in the first

two (NCYC) cycles.

4.   Maximum tolerance at the beginning is 0.15 degrees in terms of 2-

theta (TOLMX).  Only reflections with 2*obs -2*calc. <0.15 are

used to refine the cell on the first cycle.

5.   Minimum toerance is 0.03 degrees in terms of 2-theta (TOLMN).

6.   Each reflection is given a weight of 1.0. If other weight are

assigned on input, they are used for all cycles unless spec-

ified otherwise (see IWCYC on card SPACEG).

7.   Twice the standard error of an observation of unit weight is used

to obtain the value of angular tolerance, TOL.  However, TOL is

bounded by the limits TOLMX and TOLMN.

EXECUTION ON NBS' UNIVAC 1182

Interactive Mode

1.    Sign on with qualifier, POWDER

2.    Enter:  @XQT POWDER.LSQ82

3.    Enter:  DEMAND

4.    Input data following program prompts

5.    When least-squares is done, enter DEMAND for next problem or

FINISH to terminate.

Batch Mode--punch cards as follows:

1.    @RUN, M* RUNID Account, project, max time, max pages

2.    @ASG, AX POWDER*POWDER.

3.    @QXT POWDER*POWDER.LSQ82

4.    Data cards for one or more problems--first card has TITLE in

columns 1-5.

5.    FINISH

6.    @FIN

PKFILE Mode (Interactive)

1.    Sign on with qualifier POWDER

2.    Enter:  @XQT POWDER.LSQ82

3.    Enter:  PKFILE

4.    Enter:  file name following program prompt

5.    Enter:  FINISH

REFERENCES

1.  Evans, H.T.,Jr., Appleman, D.E., and Handwerker, D.S. (1973)

Report #PB216188, U.S. Dept. of Commerce, National Technical

Information Center, 5285 Port Royal Road., Springfield, VA

22151.

2.  Hess, Acta Cryst., 4, 209-15 (1951).

3.  Mighell, A.D. Hubbard, C.R., and Stalick, J.K., "NBS*AIDS80:

A FORTRAN Program for Crystallographic Data Evaluation", NBS

Technical Note 1141, National Bureau of Standards, Washington

D.C.   20234

4.  Smith, G.S., and Snyder, R.L. (1979) J. Appl. Cryst., 12, 60.

5.  de Wolff, P.M. (1968) J. Appl. Cryst.,1, 108.

6.  Young, L.C. (1941) Annals of Math. Stat., Vol. XII, 3, 293-300.

APPENDIX A

D-Spacing Generation Example

The test data listed belo show the input required for d-spacing

generation in the interactive mode (DEMAND).  The underlined items are

the required input parameters.

APPENDIX B

Least-Squares Examples

The JCPDS--International Centre for Diffraction Data Least-

Squares Task Group has surveyed available least-squares programs,

including this program.  By comparing lattice parameters and

estimated standard deviations for eleven different test data sets,

they found that most programs yielded the same results.  The

eleven test data sets and the JCPDS-NBS*LSQ82 least-squares

refinement results are given below.

The first seven test decks provide a test for the following

crystal systems:  triclinic, monolinic, orthorhombic, tetragonal,

hexagonal, rhombohedral, and cubic.  In each case unit weights

and assigned hkl were used throughout the least squares require-

ments.  Test deck #8 repeats test deck #2 (monoclinic) using hess'

weighting scheme.  Test deck #9 repeats test deck #3(orthorhombic)

with practical weights.  The practical weights are empirical and

are 1.0 unless downweighting is appropriate, because: (a) two or

more calculated 20* reflections are within 0.04 20* of the observed 20*

(b) the observed 20* was subject to possible distortion, due to

overlap with an adjacent line; or (c) *20 corr was derived by use of

etrapolated internal standard correction.  Test deck #10 adds random

noise of +0.01, 0.0, and -0.01 20* to the 20* values of test deck #2.

Test deck #11 adds randoms noise (0.01,0.00,-0.01) to the 208 values of

test deck #3.  For test deck #1, nearly complete output is shown.

For the other ten decks, IPHKL was set to two, so that only a summary

for the last cycle and a final listing were printed.  Only the summary

is included below.  Any one of the eleven test decks can be run letting

the computer assign hkl (setNOINDX=1, col 75 on card PARAMD).  Execut-

ion of test deck #B1 shows typical results.  The small differences in

refined lattice parameters between deck #1 and #B1 are due to the

exclusion from the least-squares refinement of lines with multiple index

(flag='M') possibilities.

Each example is preceeded with a listing of the test deck.  The

first line of the listing gives the test deck number (e.g.,POWDER*

LSQ82.  TESTOL on the next page).  In the example execution, the line

CADD, P LSQ82.TESTOL, for example, indicates the point of data input.