Reitveld Refinement Results (GSAS)

Sample B1 :

Phase 1 : Cinnabar (HgS) 62.511% (by wt.)

2 : Quartz (SiO2)	37.489% (by wt)

# Rwp : 11.73

2 = 1.531

All peaks  are indexed by these two phases.  There are some problems in the region of 2 11-14.5 which needs to be revisited.

Sample B3 :

Phase 1 : Cinnabar (HgS) 74.226% (by wt.)

2 : Quartz (SiO2)	25.774% (by wt)

# Rwp : 12.48

2 = 1.295

All peaks  are indexed by these two phases.  There are some problems in the region of 2 11-14.5 which needs to be revisited.

Sample B2 :

Phase 1 : Cinnabar (HgS) 12.7% (by wt.)

2 : Quartz (SiO2)	87.3% (by wt)

# Rwp : 9.69

2 = 3.72

All peaks  are indexed by these two phases.

Sample FCC4 :

Phase 1 : Cinnabar (HgS) 19.72% (by wt.)

2 : Quartz (SiO2)	80.28 %(by wt)

# Rwp : 9.97

2 = 2.965

There is slight trace of something else which has very small peaks upto 2

have put in arrows in the inset of the plot where the strongest of these peaks are.